# Text boxes

Project 1

7/27/2006 3:34:10 PM

Comment:1

Project 1

7/27/2006 3:34:45 PM

Comment:2-1

Spectrum processing :

Peak possibly omitted : 7.775 keV

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 2

Standard :

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Mg K | 0.53 | 0.44 | 0.87 | MgO |  |
| Al K | 2.54 | 1.94 | 4.81 | Al2O3 |  |
| Si K | 39.75 | 29.11 | 85.04 | SiO2 |  |
| P K | 1.02 | 0.67 | 2.33 | P2O5 |  |
| Cl K | 0.75 | 0.44 | 0.00 |  |  |
| K K | 1.49 | 0.79 | 1.80 | K2O |  |
| Ca K | 1.98 | 1.02 | 2.77 | CaO |  |
| Fe K | 1.26 | 0.46 | 1.62 | FeO |  |
| O | 50.67 | 65.13 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project 1

7/27/2006 3:34:51 PM

Comment:2-2

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 2

Standard :

P    GaP   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Cu    Cu   1-Jun-1999 12:00 AM

Ag    Ag   1-Jun-1999 12:00 AM

Pb    PbF2   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| P K | 10.95 | 11.97 | 25.10 | P2O5 |  |
| Ca K | 26.97 | 22.78 | 37.74 | CaO |  |
| Cu K | 1.62 | 0.86 | 2.03 | CuO |  |
| Ag L | 1.14 | 0.36 | 1.22 | Ag2O |  |
| Pb M | 31.49 | 5.14 | 33.92 | PbO |  |
| O | 27.83 | 58.89 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project 1

7/27/2006 3:34:58 PM

Comment:2-3

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 2

Standard :

Si    SiO2   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Si K | 46.74 | 33.33 | 100.00 | SiO2 |  |
| O | 53.26 | 66.67 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project 1

7/27/2006 3:35:12 PM

Comment:3

Project 1

7/27/2006 3:35:44 PM

Comment:4-1

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 2

Standard :

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Ti    Ti   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Mg K | 0.39 | 0.33 | 0.64 | MgO |  |
| Al K | 2.80 | 2.14 | 5.28 | Al2O3 |  |
| Si K | 39.57 | 29.04 | 84.64 | SiO2 |  |
| P K | 0.68 | 0.46 | 1.57 | P2O5 |  |
| Cl K | 0.95 | 0.55 | 0.00 |  |  |
| K K | 1.96 | 1.04 | 2.36 | K2O |  |
| Ca K | 1.78 | 0.91 | 2.49 | CaO |  |
| Ti K | 0.52 | 0.22 | 0.87 | TiO2 |  |
| Fe K | 0.93 | 0.34 | 1.19 | FeO |  |
| O | 50.43 | 64.97 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Project 1

7/27/2006 3:36:13 PM

Comment:5-1

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 2

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Ti    Ti   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.39 | 0.38 | 0.52 | Na2O |  |
| Mg K | 0.35 | 0.32 | 0.58 | MgO |  |
| Al K | 3.92 | 3.28 | 7.42 | Al2O3 |  |
| Si K | 30.83 | 24.72 | 65.95 | SiO2 |  |
| Cl K | 0.24 | 0.15 | 0.00 |  |  |
| K K | 1.38 | 0.80 | 1.67 | K2O |  |
| Ca K | 0.58 | 0.33 | 0.81 | CaO |  |
| Ti K | 0.33 | 0.15 | 0.54 | TiO2 |  |
| Fe K | 17.31 | 6.98 | 22.27 | FeO |  |
| O | 44.67 | 62.89 |  |  |  |
| Totals | 100.00 |  |  |  |  |